TYPICAL TRENCH RESTORATION IN PAVED CARTWAY N.T.S.

- Certain conditionsmay require overlay of travel line or entire street width.

See Bensalem Township Road Restoration requirements.

- Trench work must be completed at 3:30 p.m. Trench area must be secured and road reopened by 5:00 p.m. If roadway is not sevure by 5:00 p.m. contractors will incur additional consulting fees based on an hourly basis.

- Final restoration on openings for new construction shall be completed prior to occupancy. The restoration must be completed within 30 days. Failure to comply will result in a $1500 escrow in additon to any other escrow previously required.

ALL WORK TO BE DONE IN ACCORDANCE WITH PENNDOT SPECIFICATIONS

PUBLICATION 408 AS AMENDED

# Text boxes

BENSALEM TOWNSHIP

Building and Planning Department

2400 Byberry Road Bensalem, PA 19020

215-633-3644 ▪ Fax 215-633-3753

STREET OPENING

ROAD RESTORATION REQUIREMENTS

3” ID-2 WEARING COURSE

8” CONCRETE (3500 PSI)

2A

MODIFIED

STONE

6”                       6”

6”

1

ASPHALT RUBBER SEALING

COMPOUND (12” WIDE TYP.)

FINISH GRADE

COMPACT IN

6” LIFTS (MAX)

12”

12”